| R-Value and Densities Chart |  |
| --- | --- |

| Material | R-Value Per Inch | R-Value Per Unit |
| --- | --- | --- |
| Inside Air Film |  | 0.68 |
| Air Space between Studs |  | 0.95 |
| Building Paper |  | 0.06 |
| ½ in. Fiberboard Sheathing |  | 1.52 |
| Gypsum Wallboard or Drywall | 0.90 | -- |
| OSB/Particle Board - Low Density | 1.41 | -- |
| OSB/Particle Board - Medium Density | 1.06 | -- |
| Plywood or Wood Panels | 1.24 | -- |
| Hardwood | 0.90 | -- |
| Cement Mortar | 0.20 | -- |
| Sand & Gravel | 0.60 | -- |
| Stucco | 0.20 | -- |
| Glass Block | 0.51 | -- |
| Masonry Systems | R-Value Per Inch | R-V Per Unit |
| Brick 90 lb/cu ft | 0.20 | -- |
| Brick 120 lb/cu ft | 0.11 | -- |
| Concrete pour | 0.08 | -- |
| Concrete Block Normal wt. 8in. empty core | -- | 1.11 - 0.97 |
| Concrete Block Normal wt. 12in. empty core | -- | 1.23 |
| Concrete Block Medium wt. 8in. empty core | -- | 1.71 - 1.28 |
| Concrete Block Light wt. 8in. empty core | -- | 3.20 - 1.90 |
| Concrete Block Light wt. 12in. empty core | -- | 2.60 - 2.30 |
| Roofing | R-Value Per Inch | R-V Per Unit |
| Roofing Felt |  | 0.06 |
| Asphalt Roll - 90 lb | -- | 0.15 |
| Asphalt Shingle | -- | 0.44 |
| Slate ½ in. | -- | 0.05 |
| Wood | -- | 0.94 |
| Metal – any | -- | 0.00 |
| Ceramic Tile – ¼ in. | -- | 0.20 |
| Siding | R-Value Per Inch | R-V Per Unit |
| Wood Shingles 16in. – 7in. exp. | -- | 0.87 |
| Wood Drop 1in. x 8in. | -- | 0.79 |
| Wood Bevel ¾in. x 10in. | -- | 1.05 |
| Aluminum/Steel – Hollow | -- | 0.61 |
| Aluminum/Steel with 3/8in. backer | -- | 1.82 |
| Vinyl Siding | -- | <1.0 – 4.0 |
| Composite – Hardboard siding 0.4375in. | -- | 0.67 |
| Insulation | R-Value Per Inch | R-V Per Unit |
| Blankets/Batts - Fiberglass | 3.0 - 3.8 | -- |
| Blankets/Batts - Rock Wool | 3.0 - 3.8 | -- |
| Loose Fill - Cellulose | 2.8 - 3.7 | -- |
| Loose Fill - Fiberglass 0.7 lb/cu ft | 2.2 | -- |
| Loose Fill - Fiberglass 2.0 lb/cu ft | 4.0 | -- |
| Loose Fill - Rock Wool | 3.1 | -- |
| Loose Fill - Vermiculite | 2.2 | -- |
| Rigid Board - Molded Polystyrene 0.9 lb/cu ft | 3.6 | -- |
| Rigid Board - Molded Polystyrene 1.6 lb/cu ft | 3.6 | -- |
| Rigid Board - Extruded Polystyrene 1.9 lb/cu ft | 5.0 | -- |
| Rigid Board - Extruded Polystyrene - Urethanes | 5.6 - 6.3 | -- |
| Rigid Board - Extruded Polystyrene – Polyisocyanurate | 5.6 - 6.3 | -- |
| Sprayed - Cellulose | 3.0 - 4.0 | -- |
| Foam Filled - Urethane | 5.6 - 6.2 | -- |
| Vapor barrier | -- | 0.0 |

Common Rules of Thumb

| Type of Building Section | R-Value |
| --- | --- |
| Wood frame walls | 3 plus R-value of the insulation used |
| Floors above unheated spaces | 2 plus R-value of the insulation used |
| Ceilings | 1-1/2 plus R-value of the insulation |
| Single-glazed windows | 0.88 |
| Double-glazed windows | 1.67 |
| Doors with glass | Use R-value of the glass for the entire door |
| Doors without glass | 1.67 |

| Typical Masonry Systems | R-Value Per Inch | R-Value Per Unit |
| --- | --- | --- |
| Brick - 90 lb/cu ft | 0.20 | -- |
| Brick - 120 lb/cu ft | 0.11 | -- |
| Concrete Block - Normal wt. 8in. empty core | -- | 1.11 - 0.97 |
| Concrete Block - Normal wt. 12in. empty core | -- | 1.23 |
| Concrete Block - Medium wt. 8in. empty core | -- | 1.71 - 1.28 |
| Concrete Block - Light weight 8in. empty core | -- | 3.20 - 1.90 |
| Concrete Block - Light weight 12in. empty core | -- | 2.60 - 2.30 |

The following table was taken from the Home Energy Website:

| R-Values for Wall Systems |  |  |  |  |
| --- | --- | --- | --- | --- |
| No. | System Description | Clear Wall R-Value (Rcw) | Whole Wall R-Value (Rww) | (Rww/Rcw) x 100% |
| 1. | 12” two-core insulating units concrete 120lb./ft3, EPS inserts 1 7/8” thick, grout fillings 24”o.c. | 3.7 | 3.6 | 97% |
| 2. | 12” two-core insulating units wood concrete 40lb./ft3, EPS inserts 1 7/8” thick, grout fillings 24”o.c. | 9.4 | 8.6 | 92% |
| 3. | 12” cut-web insulating units concrete 120lb./ft.3, EPS inserts 2 ½” thick, grout fillings 16”o.c. | 4.7 | 4.1 | 88% |
| 4. | 12” cut-web insulating units wood concrete 40lb./ft.3, EPS inserts 2 1/2" thick, grout fillings 16”o.c. | 10.7 | 9.2 | 86% |
| 5. | 12” multicore insulating units polystyrene beads concrete 30lb./ft.3, EPS inserts in all cores | 19.2 | 14.7 | 77% |
| 6. | EPS block forms poured in place with concrete, block walls 1 7/8” thick | 15.2 | 15.7 | 103% |
| 7. | 2 x 4 wood stud wall 16”o.c., R-11 batts, 1/2" plywood exterior, 1/2" gypsum board interior | 10.6 | 9.6 | 91% |
| 8. | 2 x 4 wood stud wall 24” o.c., R-11 batts, 1/2” plywood exterior, 1/2" gypsum board interior | 10.8 | 9.9 | 91% |
| 9. | 2 x 6 wood stud wall 24” o.c., R-19 batts, 1/2" plywood exterior, 1/2" gypsum board interior | 16.4 | 13.7 | 84% |
| 10. | Larsen truss walls 2 x 4 wood stud wall 16”o.c., R-11 batts + 8-in-thick Larsen trusses insulated by 8”-thick batts, 1/2" plywood exterior, 1/2" gypsum board interior | 40.4 | 38.5 | 95% |
| 11. | Stressed-skin panel wall, 6”-thick foam core + 1/2" oriented strand board (OSB) boards, 1/2" plywood exterior, 1/2" gypsum board interior | 24.7 | 21.6 | 88% |
| 12. | 4” metal stud wall 24” o.c., R-11 batts, 1/2" plywood exterior + 1-in EPS sheathing + 1/2" wood siding, 1/2" gypsum board interior. NAHB Energy Conservation House Details. | 14.8 | 10.9 | 74% |
| 13. | 3 1/2" metal stud wall 16” o.c., R-11 batts, 1/2" plywood exterior + 1/2" wood siding, 1/2" gypsum board interior | 7.4 | 6.1 | 83% |
| 14. | 3 1/2" metal stud wall 16” o.c., R-11 batts, 1/2" plywood exterior + 1/2" EPS sheathing + 1/2" wood siding, 1/2" gypsum board interior. AISI Manual details | 9.9 | 8.0 | 81% |
| 15. | 3 1/2" metal stud wall 16” o.c., R-11 batts, 1/2" plywood exterior + 1” EPS sheathing + 1/2" wood siding, 1/2" gypsum board interior. AISI Manual details | 11.8 | 9.5 | 81% |
| 16. | 3 1/2" metal stud wall 24” o.c., R-11 batts, 1/2" plywood exterior + 1/2" wood siding, 1/2" gypsum board interior. AISI Manual details | 9.4 | 7.1 | 75% |
| 17. | 3 1/2" metal stud wall 24” o.c., R-11 batts, 1/2" plywood exterior + 1/2" EPS sheathing + 1/2" wood siding, 1/2" gypsum board interior. AISI Manual details | 11.8 | 8.9 | 76% |
| 18. | 3 1/2" metal stud wall 24” o.c., R-11 batts, 1/2" plywood exterior + 1” EPS sheathing + 1/2" wood siding, 1/2" gypsum board interior. AISI Manual details | 13.3 | 10.2 | 77% |

| DENSITY OF FRESH WATER |  | DENSITY OF SEA WATER |  | DENSITY OF ICE |  | DENSITY OF DRY AIR |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Temperature (degrees F) | Pounds per cubic foot | Temperature (degrees F) | Pounds per cubic foot | Temperature (degrees F) | Pounds per cubic foot | Temperature (degrees F) | Pounds per cubic foot |
| 32 | 62.410 | 30 | 64.250 | -50 | 57.670 | -10 | 0.088 |
| 40 | 62.418 | 40 | 64.200 | -40 | 57.625 | 0 | 0.086 |
| 50 | 62.401 | 50 | 64.170 | -30 | 57.600 | 10 | 0.085 |
| 60 | 62.358 | 60 | 64.100 | -20 | 57.582 | 20 | 0.083 |
| 70 | 62.293 | 70 | 64.020 | -10 | 57.541 | 30 | 0.081 |
| 80 | 62.208 | 80 | 63.950 | 0 | 57.105 | 40 | 0.079 |
| 90 | 62.105 | 90 | 63.800 | 10 | 57.490 | 50 | 0.078 |
| 100 | 61.986 | 100 | 63.700 | 20 | 57.455 | 60 | 0.076 |
| 110 | 61.852 |  |  | 30 | 57.410 | 70 | 0.075 |
| 120 | 61.704 |  |  |  |  | 80 | 0.074 |

Approximate values in J / kg °K of Specific Heat Capacity

| Air | 1000 |  | Lead | 125 |
| --- | --- | --- | --- | --- |
| Aluminum | 900 |  | Mercury | 140 |
| Asbestos | 840 |  | Nylon | 1700 |
| Brass | 400 |  | Paraffin | 2100 |
| Brick | 750 |  | Platinum | 135 |
| Concrete | 3300 |  | Polythene | 2200 |
| Cork | 2000 |  | Polystyrene | 1300 |
| Glass | 600 |  | Rubber | 1600 |
| Gold | 130 |  | Silver | 235 |
| Ice | 2100 |  | Steel | 450 |
| Iron, cast | 500 |  | Water | 4200 |